## Slide 1
Aktorik und Sensorik mit intelligenten Materialsystemen 2
Computer Lecture 1: Experimental Identification and Simulation of Free-Energy Function for a SMA Wire
Gianluca Rizzello
gianluca.rizzello@mmsl.uni-saarland.de Saarland University

## Slide 2: ASIM 2 - Computer Lecture 1 Overview
GOALS:
  Parametric identification of SMA free-energy function from experimental measurements
  Multi-Parabolic description of SMA free-energy function
  Simulation of temperature-dependance of free-energy function
  Simulation of the effects of external load on energy function

## Slide 3: Homework
Given an experimental SMA curve measured at T0 = 373 K, assuming ds/dT = 7 MPa/K
Calculate stress and strain from force and displacement measurements, considering a wire with initial length l0 = 142 mm and cross-section diameter d = 76 mm
Find the best single-crystal approximation which describes the experimental curve
Find the model parameters and plot the Helmholtz free-energy function y, assuming constant temperature T = T0 = 373 K
Plot the Helmholtz free-energy for different temperature values smaller than T0, showing similar trends to the ones discussed in the lecture
Plot the Gibbs free-energy g = y - se considering three different constant loads, namely s = 0.05, 0.2, 0.35 GPa (109 Pa), at T = 373 K